| ABC Petrochemicals Pvt. Ltd. | Document: INS-001 |
| --- | --- |
| Gujarat Manufacturing Plant | Rev: 1.0 ¦ Date: 15-Jan-2026 |

# Pressure Vessel Inspection  --  T-501

Equipment: T-501  --  Raw Material Storage Tank

Inspection Date: 18-Jun-2026

Inspector: Deepak Joshi (Safety Officer)

## Inspection Type

External visual inspection per API 653  --  5-year interval.

## Observations

External coating intact  --  no significant rust or peeling noted at accessible areas

Nameplate legible; last inspection date confirmed as June 2021

Stairway and platform in good condition; handrails compliant

Foundation  --  no visible settlement or cracking

Grounding cable resistance measured: 2.3 Ω (limit: < 10 Ω)

Vent piping clear; no obstruction

Overflow pipe unrestricted

## UT Spot Check Results

Bottom plate (4 spots): 7.2, 7.5, 7.0, 7.3 mm (min req'd: 6.0 mm)

Shell course 1 (4 spots): 9.8, 10.1, 9.9, 10.0 mm (min req'd: 8.0 mm)

## Conclusion

Tank T-501 is in satisfactory condition. All measured thicknesses exceed minimum required values. Next full inspection due: June 2031.

Inspector: Deepak Joshi  |  Signature: dj/t501/18jun26